## Slide 2: Theory
Express and in terms of and
The single diode equation
Solving equation 1 for and
Solving equation 1 for and

## Slide 3
Combine equation 2 and 3 to obtain equation 4 and 5
If the term
Equation 5 can be reduced to

## Slide 4
Extracted Parameters |  | 
Rs (Ω) | Rsh (kΩ) | n
-1.28 | 10.00 | 2.88
What is the problem?

## Slide 5
Current models for characterization are not reliable enough for high throughput characterization
  Negative parameters
  Initial guesses in literature are not applicable for all I-V data curves
    Too far from the actual solution
    Undefined at initial guess
  Non realistic parameters extracted
Solutions to these problems mean
  More accurate and reliable parameter extraction
  Help understand the issue causing low fill factor
Problem Statement

## Slide 6
Hypothesis
Applying constraints to the possible and will improve the accuracy of the extracted parameters.

## Slide 7
Objectives
Investigate the ability of the model to extract accurate and sensible and for different IV data
  Compare extracted parameters with actual parameters
  Test robustness of the model with experimental data

## Slide 8
Simulate IV data
Generate evenly spaced voltage data from to .
Generate current with explicit single diode equation.
Introduce noise with signal to noise ratio (SR) of 45
Specify the following

## Slide 9: Simulated cases
Case | Rs (Ω) | Rsh (kΩ) | n
1 | 0.10 | 1.00E+03 | 1.00
2 | 25.00 | 1.00E+03 | 1.00
3 | 0.10 | 0.20 | 1.00
4 | 0.10 | 1.00E+03 | 2.50
5 | 25.00 | 1.00E+03 | 2.50
6 | 0.10 | 0.20 | 2.50
7 | 0.10 | 1.00E+03 | 5.00
8 | 25.00 | 0.20 | 5.00
Specify the following
= 1V
= 20 mA
= case(i,2)
= case(i,3)
= case(i,4)

## Slide 10: Simulated cases 1 - 4
Case | Rs (Ω) | Rsh (kΩ) | n
1 | 0.10 | 1.00E+03 | 1.00
2 | 25.00 | 1.00E+03 | 1.00
3 | 0.10 | 0.20 | 1.00
4 | 0.10 | 1.00E+03 | 2.50

## Slide 11: Simulated cases 5 - 8
Case | Rs (Ω) | Rsh (kΩ) | n
5 | 25.00 | 1.00E+03 | 2.50
6 | 0.10 | 0.20 | 2.50
7 | 0.10 | 1.00E+03 | 5.00
8 | 25.00 | 0.20 | 5.00

## Slide 12: Parameter extraction (1): Gradients at and
2) Find and from data
3) Find and
4) Fit data with two 2nd order polynomials
1) Smooth current data
5) Differentiate 2nd order polynomial
6) Evaluate polynomials at I = 0 and

## Slide 13: Parameter extraction (2) : Initial guesses

## Slide 14
can be retrieved by substituting the calculated in into equation (5). Equation (5) has been rearranged below to make as the subject of the formula.
Equation 6 and 5 can be subtracted to obtain to as function of known parameters.

## Slide 15: Parameter extraction (3): Solver Setting
Use MATLAB built in ‘lsqnonlin’ function
  Algorithm - trust region method
Tolerances =
Minimize least squares data in the active quadrant
Constraint the possible solutions of and

## Slide 16: Analysis
Compare extracted parameters with actual parameters
Test robustness of the model on experimental data

## Slide 17: Results
Simulated IV characterization
Literature IV characterization
Research solar cells characterization

## Slide 18: Simulated case 1 - 4

## Slide 19: Simulated case 5 - 8

## Slide 20: Simulated results
Case | Rs |  |  | Rsh |  |  | n |  |  | RMSE
 | Actual | Extract | %Error | Actual | Extract | %Error | Actual | Extract | %Error | 
1 | 0.10 | 0.07 | 33.08 | 1.00E+06 | 4.18E+04 | 95.82 | 1.00 | 1.00 | 0.00 | 1.32E-04
2 | 25.00 | 25.05 | 0.21 | 1.00E+06 | 4.22E+03 | 99.58 | 1.00 | 1.00 | 0.00 | 4.41E-05
3 | 0.10 | 0.00 | 99.90 | 2.00E+02 | 2.08E+02 | 3.85 | 1.00 | 1.06 | 5.53 | 1.12E-04
4 | 0.10 | 0.14 | 40.15 | 1.00E+06 | 6.63E+03 | 99.34 | 2.50 | 2.45 | 1.80 | 5.23E-05
5 | 25.00 | 25.22 | 0.86 | 1.00E+06 | 4.58E+03 | 99.54 | 2.50 | 2.42 | 3.09 | 3.20E-05
6 | 0.10 | 0.02 | 79.86 | 2.00E+02 | 2.02E+02 | 0.78 | 2.50 | 2.53 | 1.24 | 4.11E-05
7 | 0.10 | 0.53 | 426.42 | 1.00E+06 | 3.11E+04 | 96.89 | 5.00 | 4.72 | 5.55 | 7.62E-05
8 | 25.00 | 25.02 | 0.06 | 2.00E+02 | 2.09E+02 | 4.70 | 5.00 | 5.00 | 0.01 | 2.79E-05
Case 1 has highest RMSE in all cases
  More noisy data
Large %error for high Rsh and low Rs
Low %error for n
RSME is not ultimate indicator of accuracy
  Observe case 3 and 1

## Slide 21: Fitting silicon solar cell IV data
Experimental data from a 57 mm diameter commercial (R.T.C France) silicon solar cell at 33 C.

## Slide 22: Comparing Bee Swarm Method with this model
Rs |  |  | Rsh |  |  | n |  |  | RMSE |  | 
This method | Modified bee swarm | %Error | This method | Modified bee swarm | %Error | This method | Modified bee swarm | %Error | This method | Modified bee swarm | %difference
0.043 | 0.036 | 17.34 | 43.71 | 53.40 | 18.15 | 1.43 | 1.48 | 3.48 | 2.50E-03 | 9.86E-04 | 86.85

## Slide 23: Fitting perovskite solar cells